## Slide 1
Pritchard, Christopher D., et al. "An injectable thiol-acrylate poly (ethylene glycol) hydrogel for sustained release of methylprednisolone sodium succinate." Biomaterials 32.2 (2011): 587-597.
Factors That Influence Successful Base Catalyzed Thiol-ene Hydrogel Synthesis
Nolan J. Morrison and Brandon M. Vogel Department of Chemical Engineering, Bucknell University, Lewisburg, PA.
Abstract
References
Acknowledgements
Precursor Purification
ETTMP and PEGDA passed through separate purification columns and Büchner flasks
Mass ETTMP = 2x Mass Alumina
Future Work
Background
A hydrogel is a network of crosslinked polymer chains swollen in water
ETTMP-PEGDA hydrogels form their network through a Conjugate Michael Addition reaction
PEG hydrogels don’t require light or heat to cure, giving them the ability to be injected
Goals
Develop a reproducible procedure to synthesize ETTMP-PEGDA hydrogels
Provide a sensitivity analysis of major variables that impact successful synthesis
Quantify mechanical properties as a function of polymer concentration
Determine optimal conditions for long-term storage of gel mixtures
Motivation
Increase efficiency and reproducibility of synthesis method
Develop a reliable, injectable drug delivery platform
Introduction
Ethoxylated trimethylolpropane tri-3-mercaptopropionate (ETTMP) and poly(ethylene glycol) diacrylate (PEGDA)-based hydrogels are a promising candidate for injectable, localized drug delivery due to the potential for non-swelling behavior and controllable drug release properties. However, we find that existing literature synthesis methods suffer from slow gelation times or a lack of reproducible procedures. In this work, we present a repeatable synthesis procedure, along with a sensitivity analysis of the major variables that impact successful synthesis. Our methods allow the hydrogels to be reliably synthesized in a polymer concentration range of 15 to 90 wt.%, resulting in gelation times between 2 min and 1 h with equilibrium moduli between 3.5 and 190 kPa. Furthermore, base-catalyzed conjugate Michael curing led to 16.35 min and 1.67 min gelation times for buffer pH values of 6.5 and 8, respectively. Additionally, we show that ETTMP purification directly controls the concentration of mercaptopropionic acid (MPA) necessary to inhibit the Michael addition. Lastly, we find that a stoichiometric mixture of ETTMP and PEGDA has a freezing point range of -17.9 ºC to -27.2 ºC and can be stored at -20 ºC for 2 months without crosslinking, as opposed to 2 days at room temperature, making storage and shipment of mixtures possible.
Conclusion
Results and Discussion
Methods
Bucknell University Department of Engineering
Professor Brandon M. Vogel
Diane Hall, Chemical Engineering Lab Director
Vogel Research Group
Quantify the rate of erosion in phosphate buffered saline
Study the controlled release of a Rhodamine 6G loaded hydrogel
Determine the cytotoxicity of the hydrogels
Develop strategies to control the erosion and release rates
Hydrogel Synthesis
Mix ETTMP, PEGDA, and PBS according to 2:3 stoichiometric ratio
259 μL ETTMP
180 μL PEGDA
1500 μL PBS
(25 wt% solids)
Figure 1. Conjugate Michael Addition reaction for the
crosslinking of ETTMP and PEGDA
Figure 2. Precursor purification schematic
Figure 3. A 2 gram, 25 wt% hydrogel before and after undergoing conjugate Michael addition
Mechanical Properties and DSC Results
Figure 4. Change in gel time as a function of buffer pH. Hydrogels with 25 and 35 wt% polymer concentrations were tested.
Figure 5. Change in gel time and MPA concentration as a function of purification column height. Hydrogels with 25 and 35 wt% polymer concentrations were tested.
Table 1. Mechanical property data for hydrogels synthesized with polymer concentrations ranging from 15 to 90 wt%.
Figure 6. DSC thermograms of ETTMP, PEGDA, and a stoichiometric mixture of ETTMP and PEGDA. Samples were equilibrated at 35 ºC then cooled at a constant rate of 10 ºC/min.
Effect of pH and Purification Column Height
Decreasing pH results in a near-exponential increase in gel time
Purification directly controls the concentration of MPA in ETTMP and, thus, the gel time
Our method allows for a wide range of polymer concentrations
Stoichiometric ETTMP-PEGDA mixtures have a freezing point range of -17.9 ºC to -27.2 ºC
Frozen mixtures can be stored at -20 ºC for up to 2 months, then used for synthesis once thawed
Notes: Make legend larder and bold
Add references
Make conclusion sound better
Labels in column figure bold and bigger